## Slide 1: Thermal Hardware Introduction David Steinfeld NASA Goddard/ Code 545
Presented By David Steinfeld
Thermal & Fluids Analysis Workshop TFAWS 2023 August 21-25, 2023
NASA Goddard Space Flight Center
College Park, MD
TFAWS Passive Thermal Paper Session

## Slide 2: David’s Bio
Education:
  Georgia Tech
    1985 Bachelors Degree Mechanical Engineering
  University of Texas, Arlington
    1989 Masters Degree Aerospace Engineering
Employment:
  1985-1999: LTV Aerospace and Defense, Dallas TX
    Space Shuttle Carbon-Carbon Leading Edges Reentry heating
    Space Station (ISS) Radiators (HRS, Photovoltaic, Solar Dynamic)
  1999-Pres: NASA Goddard Space Flight Center, Greenbelt, MD
    Chief Engineer Thermal Engineering Branch
    Worked many space missions, including Hubble Telescope and its servicing missions, Triana, SDO, LRO, MMS, STEREO, LUCY, Landsat-9, ExoMars/MOMA, DAVINCI, Dragonfly/DraMS

## Slide 3: Topics
MLI Blanketing Theory 101
MLI blanketing installation
Temperature Measurements
Heaters and Thermostats
Optical coatings (Paints and tapes)
Interface Conductance and Gap fillers
Ordering Flight Hardware
Louvers

## Slide 4: MLI Blanketing 101
Thermal Analyst:
“The actual MLI doesn’t look like my Thermal Desktop Model”
Blanket Tech:
“David, can you help me out? The Thermal Analyst
can’t tell me what he wants”

## Slide 5: Thermal Model vs. Hardware
Thermal Model
Actual MLI
STEREO/PLASTIC as an example

## Slide 6: Actual vs. Theoretical MLI Blanket
Chart: MLI Blanket Effectiveness (Large, Flat Blanket)
| 1 | 2 | 5 | 10 | 15 | 20 | 50
ε-star | 0.05 | 0.0085 | 0.0035 | 0.0024 | 0.0017 | 0.0013 | 0.0005
Actual Blanket | 0.027 | 0.015 | 0.01 | 0.007
Theoretical MLI
Actual MLI

## Slide 7: What effects MLI blanket ε*?
Penetrations
Ground Straps
Crinkling
Stitching
Vents
Separator layers
Tightness
Cryogenic Temperatures
Atmospheric pressure

## Slide 8: What effects Optical Properties?
Emissivity usually not effected by age (BOL vs. EOL), its already high.
Alpha increases with age (BOL vs. EOL)
  It darkens
Atomic oxygen effects outer layer
  Silver Teflon needs to be 10 mil instead of 5 mil thick in LEO

## Slide 9: MLI Layers Touching = Bad
For every 1 ft2 blanket covering a 30OC surface:
  Good MLI blanket design = 1.2 watts lost
  Smashed blanket = 38.0 watts lost

## Slide 10: Stitching Effects 1 ft wide blanket
Chart: Distance (in)
| 0 | 1 | 1.9000000000000001 | 4 | 6 | 8 | 10.1 | 11 | 12
E-star | 0.148 | 0.05 | 0.025 | 0.017 | 0.015 | 0.017 | 0.025 | 0.05 | 0.148
SEAM
SEAM

## Slide 11: Blankets Vent or Blow Up
Air Pressure on ground
  14.7 psi
  2117 lbs per square foot.
  But pressure in Space = 0 psi.
Blankets go from Ground to Space pressure (or inside T/V chamber)
  Air around MLI goes from 14.7 psi -> 0 in about 120 seconds
MLI Blankets can only handle 0.1 psi (14.4 lbs per square foot)
Venting needed:
  Between MLI layers (or risk blowing up)
  Between MLI and underlying substrate (or risk being blown off surface)
  Eliminate Gas conduction

## Slide 12: Generic Launch Pressure Inside Fairing
Chart: Time (Sec)

## Slide 13: Cryogenic Temperatures effect MLI Blankets
Chart: Temperature (C)
| 0 | -73 | -123 | -173 | -198 | -213
e | 0.0007 | 0.001 | 0.0017 | 0.0038 | 0.008 | 0.012
Emissivity shifts to the far infrared
at very cold temperatures.

## Slide 14: Things Grow and Shrink
Coefficient of Thermal Expansion
  Things grow bigger when hot
  Things shrink when cold
  Aluminum shrinks/grows a lot compared to Kapton
    CTE = 0.000026 in/in OC
    72 inch Bus Panel, from -20 OC to +40 OC grows 1/8”
Metal
MLI
Blanket Buttons

## Slide 15: Blanket Buttons, Etc…
Top hat
Blanket buttons
Velcro

## Slide 16: ClickBonds (For heavier or thicker blankets)

## Slide 17: Bonding Thermal Hardware
Thermofoil (Kapton) Heaters
  Under 3.5 w/in2: 3M 966 Acrylic adhesive
  Over 3.5 w/in2: Stycast 2850FT
Thermal Hardware (MLI Buttons, Thermistors, PRTs, Thermostats) bonded with Stycast 2850FT Catalyst 9
  Small bondline, so thermal resistance is low.
Polymerics license required for bonding Flight hardware.
Surface preparation is key to a good bond:
  Clean surfaces
  Abrade surfaces with sandpaper
  Vacuum, then clean surface again
  Hold down with Kapton until epoxy dries overnight.
    Think about how to handle vertical surfaces!

## Slide 18: Temperature Measuring Devices
Thermocouple
  Only used for thermal vacuum testing
  Typically bought in a large length spool
    Omega Engineering a good source
  Cut to length, solder the bead
Thermistor
  Resistance of the bead changes with temperature
  Flight units bought from:
    TE Connectivity (Measurement Specialties, Inc)
    QTI (Boise, ID)
PRT
  Used for high or low (cryogenic) temperatures
  Flight units bought from:
    UTC Collins Aerospace (formerly Rosemount)
    QTI (Boise, ID)
Thermistor
PRT
Thermocouple

## Slide 19: Thermocouples
Used for Thermal vacuum testing
  Not used for Flight, but sometimes may fly…
Two dissimilar metals create a voltage difference
  Seebeck Effect
  Voltage dependent on temperature
Cheap to purchase
Quick to install
  Attached with Aluminum tape
Very long lengths allowed
  75 feet not uncommon
Need complicated (expensive) electronics to read temperature
Different metal combinations:
  Type T (Red + Blue) is normal at Goddard (-200C to +350C)
    Copper-Constantan
  Type K (Red + Yellow) used for higher temps (-200C to +1250C)
    Chromel-Alumel

## Slide 20: Thermistors
Resistance changes with Temperature
  Metal oxide bead material
Very non-linear response
  Negative slope curve
    NTC (Negative Temperature Coefficient)
  Comes in various resistances
  2252 Ω, 1000 Ω, 5000 Ω, 10,000 Ω, etc…
  Nominal resistance rated @ 25OC
  Temperature range -55C and +90C
    Not to be used on solar arrays or cryogenic applications
    High temp exposure permanently changes resistance of the bead

## Slide 21: Thermistor Specs
  Thermistors:
    S-311-P-18L: Standard GSFC thermistor
    S311-P-8-827A: QTI surface mount (chip style)

## Slide 22: Thermistor Part Number
Correlation between manufacturer number and Goddard number

## Slide 23: PRTs
Resistance element is Platinum
  Platinum Resistance Thermometer
Positive slope
  PTC (Positive Temperature Coefficient)
Very linear Temperature vs. Resistance curve
Temperature range -269OC to 400OC
  Others capable up to +800OC,
  Nominal resistance rated @ 0OC
4 wire variety enhances accuracy if needed
  Removes resistance of leads.
  Resistances usually 100 Ω

## Slide 24: 2 PRT Packages
Wire wound
  Cylindrical shape package
  Platinum wire wrapped around a spool
  Not vibration resistant
  More accurate at high/low temps
  10X more expensive than thin film
Thin film deposition
  Rectangular shape package
  Platinum is deposited onto a ceramic substrate
  Better for high vibe loads
  Less accurate at high/low temps
    Temperature change will grow/shrink package; slightly changing resistance due to strain

## Slide 25: Mechanical Thermostats
Flight qualified vendors: from Honeywell, Sensata, or Comepa
  NASA Goddard S311-641 specifications
  Honeywell Type 700
  Sensata M1, M2, 3BT, 4BT
  Comepa has an ESA Spec which Goddard agreed to allow as a S311 surrogate
Style 701, or M1 (standard)
Style 717 (Prop lines)
Sensata Style 3BT

## Slide 26: Sensata M1 and M2 Thermostats (1/2” disks)
M1: Large Temp Differential
  20OF (9OC)
-65°F to 550°F (-53.9°C to 287.8°C) close setpoints
5amps @ 30 VDC
  100,000 cycles minimum
M2: Small Temp Differential
  2°F to 5°F (1.1 to 2.8°C)
-40oF to +235oF (-40oC to 112.8oC) close setpoints
2.0 amperes at 30Vdc, 250,000 cycles
3.0 amperes at 31Vdc, 50,000 cycles

## Slide 27: Thermostat Specs for Flight Hardware
  Thermostats:
    NASA S-311-641-XX
      B: General Requirements
      /02: Sensata M2 (narrow differential)
      /03: Honeywell 700 Series (standard t’stat)
      /04: Honeywell 270 Series (High Power, 10amp)
      /05: Sensata M1 (large differential)
      /06: Sensata 4BT (super tiny)
      /07: Sensata 3BT (super tiny)

## Slide 28: S311-P641/03 Spec

## Slide 29: Heaters
Kapton (Polyimide) Thermofoil Heaters
Typically applied with 3M 966 Acrylic Adhesive
  Low outgassing
Kapton material temp limit +150OC (although Minco makes some good to +200OC)
  966 adhesive good to about +130OC (data sheet says +204OC) before outgassing happens
  Bond with Stycast Epoxy if hotter than +130OC, or watt density higher than 3.5 W/in2
Overtaped with 3M 425 aluminum tape to help spread out heat from potential “bubbles”
  Note: Be careful when bonding heaters to cylindrical surfaces with 3M966 (spring-back)

## Slide 30: Heater-Thermostat Redundancy
  Two thermostats wired in series
    To prevent failed “on” condition
  Two heaters wired in parallel
    To prevent failed “off” condition
  Heaters can be ordered with dual-elements
    Cost is about the same as single element
    Remember to order heaters with two color coded wires (to tell circuits apart)
-
Thermostats 1,2
-
Primary
Redundant
Heater 1
Heater 2
Thermostats 3,4
+
+

## Slide 31: Heater Specs
Heaters:
  Procurement: S-311-P-079
    Order to this spec.
  General Specifications: S-311-P-841
    Tells how the heater should be made

## Slide 32: Optical Coatings
Word of Advice: Never call an optical coating “Paint”!
Things that effect Optical coatings:
  Atomic Oxygen*
  UV Radiation*
  Proton-Electron particle Radiation
  Contamination on the surface
  Note: * LEO orbits
Example: Silver Teflon in LEO usually needs 10mil Teflon instead of 5 mil (AO erodes the Teflon)

## Slide 33: Optical Coatings, Page 2
Thickness of the coating is key:
  Too thick makes the coating crack
  Too thin effects the emissivity and solar absorptance
Coating Selection
  The Substrate: metal or composite?
  Temperature range:
    Polyurethanes do not do well at hot temperatures. They turn brown.
    Silicates work better when hot but have their own problems.
Coat on flat side of the radiator, not on pocketed side if possible.
Fillets and bolt patterns create 5-10X more time to coat. $$$$
Talk to your Coatings Engineer before you get too far down the path.

## Slide 34: Contact Conductance in a Vacuum: “Potato Chipping” between bolts
Conduction Highly dependent upon:
Box baseplate thickness
Distance between bolts
Bolt diameter
Bolt Torque
Stiffness of Coldplate/radiator
Overall Dimensions of box.
No Contact

## Slide 35: Solid Sheet Thermal Enhancement
Chotherm 1671
  Non electrically conductive
  15 mils thick
Choseal 1285
  Electrically dissipative
  20 mils thick
e-Graf
  5 or 10 mils thick

## Slide 36: Liquid Thermal Enhancement
Nusil CV-2946
  2-part material which needs to be mixed beforehand and degassed.
  Stored in a freezer or hardens in an hour
  Use Miller-Stephenson MS-143H as a release agent if needed. Teflon particles. Apply 3 layers.
Arathane
  Mixed with 30-40% Boron Nitride increases thermal conductivity.
  Cabasil makes it thick.

## Slide 37: Results for an 8” X 8” Ebox
Empirical G = 0.10 W/in2-C
Datasheet G = 4.35 W/in2-C
Datasheet G = 1.59 W/in2-C

## Slide 38: Louvers
Louvers have been used since the 1950’s
  Hundreds/thousands used on satellites
  Not aware of any failures
Thermally activated shutters regulate the structural/electronic equipment temperature
Highly-polished aluminum blades driven by bi-metallic sensors
  Totally passive; No heaters needed
Open when hot. Closed when cold
Typical thermal performance:
  Open ε*=0.70
  Closes ε*=0.09

## Slide 39: End of Class
Any last questions?