## Slide 1: Epoxy, Heaters, Sensors and Wiring NASA-GSFC
Presented By Colton Cohill
Thermal & Fluids Analysis Workshop TFAWS 2023 August 21-25, 2023
NASA Goddard Space Flight Center
College Park, MD
TFAWS Thermal Instrumentation Paper Session

## Slide 2: About me
  Thermal technician at NASA GSFC for the past 7 years.
  Supporting Roman Space Telescope (RST) and various flight projects with thermal hardware applications.
  Hold certifications for ESD monitoring, J-STD Soldering, Polymerics, Crimp ,Cable and Harnessing.
  I do most of my work in our branch thermal lab which consist of installing hardware for various projects into chambers simulating the vacuum pressure in space.
  Preparing the tests by interfacing electric heaters, cooling lines, sensors, blankets and communication cables.

## Slide 3: 4 Different Thermal Hardware Installs
Heaters
  3M966 Acrylic Adhesive if watt density is less than 3.5 W/in2
  Stycast Epoxy if watt density is greater than 3.5 W/in2
Thermocouples
  Usually aluminum tape
Thermostats, Themistors, PRTs
  Stycast Epoxy
Nusil under an Ebox
  If watt density is so high, solid gap fillers won’t work

## Slide 4: Who can do the work?
For Flight hardware, a Polymerics License is REQIRED
  Many hours of class
  Recertification every 2 years
No Polymerics license, Do not touch Flight Hardware!!!
  I have a license 

## Slide 5: Types of Material
Thermal adhesive transfer tape
  966 Pressure Sensitive Adhesive (PSA)- operating temperature
  232 ̊c to -40 ̊c (we’ve proved it works down to -40K)
Thermal epoxy bond
  Stycast/catalyst 23LV- operating temperature -65 ̊c to 105 ̊c (Room temp. cure, 16 to 24 hours at 25 ̊c)
  Stycast/catalyst 11LV- operating temperature -55 ̊c to 155 ̊c (Heat to cure, 8-16 hours at 80 ̊c)
  Stycast/catalyst 9LV- operating temperature -40 ̊c to 130 ̊c (Room temp. cure, 16 to 24 hours at 25 ̊c)
Thermal elastomer interface
  Nusil CV1-2946- for thermal conductivity wet joint
  To cure 7 days minimum at ambient temperature and humidity
  Operating temperature -50 ̊c to 250 ̊c
  Miller Stephenson- semi-permanent mold release

## Slide 6: Heaters
How HEATERS are installed

## Slide 7: Applying PSA
  Abrade your heater with fine grit Scotch-Brite
  Frame the bonding area with tape to prevent unintended damage to the surrounding area.
  Any surfaces with a coating such as paints must be removed by Abrasion using sandpaper.
  Remove the tape framing.
  Clean the abraded and surrounding area very carefully with IPA
  Allow the hardware to dry.
  Apply PSA to the heater and then apply heater the substrate.
Notes: we mask the location of the with 2 layers of aluminum or Kapton tape leaving 1/8in on each side for a fillet.

## Slide 8: Surface preparation for bonding
  Frame the bonding area with tape to prevent unintended damage to the surrounding area.
  Any surfaces with a coating such as paints must be removed by Abrasion using sandpaper.
  After abrasion remove the framing tape.
  Clean the abraded and surrounding area very carefully with IPA
  Allow the hardware to dry.
  Following the work instruction 541-WI

## Slide 9: Bond height & Applying Epoxy
  Add the desired amount of aluminum tape for the bond height
  Add your epoxy and smooth it out using the tape as a guide rail
  Separately on a clean surface like a sheet of aluminum foil repeat step for the heater being used
  Once both surfaces have been wetted with epoxy they can be joined
Notes: we mask the location of the with 2 layers of aluminum or Kapton tape leaving 1/8in on each side for a fillet.

## Slide 10: Setting a heater
  Once you have a smooth layer on each surface you will want to remove all aluminum tape.
  Once the tape has been removed you will place the heater on to the substrate.

## Slide 11: Applying weight
  Once you have the heater on the substrate you will add leveling plate.
  This plate will be made up of layers.
  The first layer will be Teflon tape to hold a rubber pad to a 1/8” aluminum plate and then placing a two-pound weight on top.

## Slide 12: Thermocouples
How Themocouples are installed

## Slide 13: Thermocouple Installation
Thermocouples are temporary during TVAC testing
  Need to stay in place, but removeable after the test
  Aluminum Tape (3M425) is standard method
  Label T/C bead and miniplug with a vacuum compatible numbers
  Bend Thermocouple into a “U” shape
  Apply aluminum tape over T/C bead
  Burnish Aluminum tape down with a Teflon Stick, etc…

## Slide 14: Thermostats, Thermistors, PRTs
How Tstats, thermsitors, PRTs are installed

## Slide 15: Applying a Thermistor and PRT
  Abrade the location for the sensor and clean with IPA
  Add tape to hold the sensor in place while epoxy dries
  Add a small bead to the surface under and over the sensor
  You can stake the sensor in place with arathane
Notes: we mask the location of the with 2 layers of aluminum or Kapton tape leaving 1/8in on each side for a fillet.

## Slide 16: Eboxes
How Eboxes are installed with Nusil

## Slide 17: Desired height & Applying Nusil
  Clean your mounting surface with IPA and allow to dry.
  Add a mold release agent to the Radiator/cold plate
  Add the desired amount of aluminum tape for the bond height.
    5 mils thick per layer
  Add Nusil to the Ebox and smooth it out
  Join the electronics box to the mounting surface.
Notes: we mask the location of the with 2 layers of aluminum or Kapton tape leaving 1/8in on each side for a fillet.

## Slide 18: Lessons Learned & Possible Issues
Bonding issues
  Accidentally creating bubbles or voids in epoxy.
  Bubbles or voids can create hot spots and burn out the heater.
  PSA (pressure sensitive adhesive tape) when applied incorrectly can have bubbles or may not fully cover heater surface.
  Epoxy can run when applied to a vertical surface, depending on the fluid consistency.
  Bonding onto a curved surface can be difficult if a heater is not pre-formed prior to applying.
    Heater can spring back
    Flight qualified Zip Ties help hold it on if needed.