## Slide 1: Hydrophobicity of Cryogenic Fluids for Fuel Transfer in Space Applications
Martin Rosales
Eduardo J. Bidot-Lopez
Matthew Wittal
Intern, NASA Deep Space Logistics
Intern, NASA Deep Space Logistics
GN&C Engineer, NASA Deep Space Logistics

## Slide 2: Background and Motivation
Fuel flow is important for rocket performance
Increasing fuel flow can increase performance/efficiency
Inducing a hydrophobic surface on the interior surfaces of the fuel tanks/fuel lines
  Reduces friction
  Increases flow rate

## Slide 3: Cryogenics
Behavior of materials at very low temperatures
  ~<-100°C
  Space is inherently cryogenic
  Cryogenic fluids are commonly used as spacecraft fuel
    Usually diatomic
    Nonpolar

## Slide 4: Hydrophobicity

## Slide 5: Methods of Hydrophobicity
Physical
  Surface quality
  Can be applied to various materials and/or surfaces
Chemical
  Polarity
    Opposite polarities repel, being “hydrophobic”
  Inherent property of substances
Repels

## Slide 6: Assumptions
Determine hydrophobic properties at cryogenic temperatures
  Etched wafer testing
  Preliminary chemical coating testing
    Determine if chemical hydrophobicity remains constant with different states of matter
    Determine if this hydrophobicity remains constant at cryogenic temperatures

## Slide 7: Testing Apparatus

## Slide 8: Testing Procedures
Pour over cryogenic fluid to reduce the temperature of the wafer
Allow for the boil off to expose wafer
  Wafer should be the same temperature as the cryogenic fluid
Use dropper and drop cryogenic fluid on wafer (at cryogenic temperatures)

## Slide 9: Etched Wafer Testing Results
Tested LN2 & LAr
  LAr > LN2
  Other cryogenic fluids pose unique issues
    LH2
    LOx
Minimal wetting angle
Mostly hydrophilic

## Slide 10: Preliminary Chemical Results
Solid nonpolar substance, liquid polar substance
  Tested at room temperature
Extremely hydrophobic
  Hydrophobic properties remained constant with different states of matter

## Slide 11: Discussions
Etched wafer still has promise, depends on properties of the etch
  Depth
  Width
  Pattern
Chemical has greater promise
  Solid lipid and water used
  Polar repels nonpolar regardless of state of matter
  Lithium stearate

## Slide 12: Future Work
Etched Wafer
  Alternate etching patterns
  Alternate materials
Chemical testing
  Advancing chemical testing to lithium stearate and cryogenic fluids
  Coat surface with lithium stearate and replicate etched wafer testing procedures
  Alternate coatings
Induced Current
  An alternating current across the surface could induce hydrophobicity

## Slide 13
Key References:
J. Narbutt, “Chapter 4 - fundamentals of solvent extraction of metal ions,” in Liquid-Phase Extraction (C. F. Poole, ed.), Handbooks in Separation Science, pp. 121–155, Elsevier, 2020.
A. Y. Vorobyev and C. Guo, “Multifunctional surfaces produced by femtosecond laser pulses,” Journal of Applied Physics, vol. 117, p. 033103, 01 2015.
P. P. Madeira, G. Todorov, V. N. Uversky, and B. Y. Zaslavsky, “Solvent polarity and hydrophobicity of solutes are two sides of the same coin,” Biochemical and Biophysical Research Communications, vol. 701, p. 149600, 2024.
B. Zohuri, “Chapter 1 - cryogenic technologies,” in Physics of Cryogenics (B. Zohuri, ed.), pp. 1–51, Elsevier, 2018.
G. Klesse, S. J. Tucker, and M. S. P. Sansom, “Electric field induced wetting of a hydrophobic gate in a model nanopore based on the 5-ht3 receptor channel,” ACS Nano, vol. 14, no. 8, pp. 10480–10491, 2020. PMID: 32673478.
Thank you! Questions?
Contact:
Martin M. B. Rosales | Matthew Wittal
martinmbrosales@gmail.com | matthew.m.wittal@nasa.gov