## Slide 1: Boundary Layer Characterization around Graphite Samples in Microwave Nitrogen-Methane Plasmas
Dan Fries*, William L. Young*, Kate B. Rhoads*, Savio Poovathingal*, Alexandre Martin*
Stefan Löhle**
NASA TFAWS Aero-VI-03 ∙ August 5th , 2025 ∙ San-Jose, CA
*University of Kentucky
**University of Stuttgart

## Slide 2: Introduction & Motivation
NASA Dragonfly mission will explore the Saturn moon Titan in great detail.
A safe entry into Titan’s atmosphere is critical
Atmosphere is mostly nitrogen and methane [1]
Cassini-Huygens is the only existing flight data set for this kind of atmosphere [2]
Ground tests are needed to understand the reentry-environment better and to reliably predict radiative heat transfer and dominant chemical pathways
Data will be used to validate and improve modeling tools for Dragonfly and other missions [3]
Source: NASA
Objectives:
Perform material tests in 98.5% N2 + 1.5% CH4 high-enthalpy gas mixtures
Spectroscopic characterization of the radiative environment
Description and validation of gas-material interaction models
[1] Nixon, “The composition and chemistry of titan’s Atmosphere”, ACS Earth Space Chem. (2024).
[2] Johnston and Brandis, "Analysis of Huygens Entry Observation to Inform Titan Shock-Layer Radiation Models." J. Thermophysics and Heat Transfer (2022).
[3] Brandis et al., “Mitigating dragonfly TPS design risks through improved aerothermal environments”, 2024 IPPW (2024).
NASA, JPL-Caltech and University of Arizona
Source: NASA, JPL-Caltech and University of Arizona

## Slide 3: Experimental Setup & Methodology
Local Heat Transfer Simulation Methodology to identify relevant geometries and flow conditions [1]
 | HELMUT | Titan
Altitude | - | km
Total pressure | mbar | mbar
Density | kg/m3 | kg/m3
Velocity | m/s | m/s
Total enthalpy | MJ/kg | MJ/kg
Mach # |  | 
Dragonfly radius | mm | mm
 | HELMUT | Titan
Altitude | - | 
Total pressure |  | 
Density |  | 
Velocity |  | 
Total enthalpy |  | 
Mach # |  | 
Dragonfly radius |  | 
[1] Kolesnikov, "The concept of local simulation for stagnation point heat transfer in hypersonic flows-applications and validation." 21st Aerodynamic Measurement Technology and Ground Testing Conference (2000).
UK High-Enthalpy Multi-User Test (HELMUT) Facility: microwave plasma, variable pressure
Use solid POCO graphite as representative material
HELMUT
POCO graphite sample

## Slide 4: Experimental Setup & Methodology
Targeting laser from the spectroscopy system
Broadband low-resolution spectroscopy diagnostic
Measurement radius at focus mm, sr  approximate line-of-sight
Calibrated with tungsten-halogen and deuterium radiance standard
Looking through strong CN radiation in gas phase
Instrument function

## Slide 5: POCO Samples Exposed to Plasma Stream
Violet glow close to surface  CN
CN in bulk plasma
1) Exposed once for ~5 min, [CH4] nominal
2) Exposed once for ~10 min, [CH4] of 1)
3) Exposed once for total >10 min, [CH4] of 1)
pure N2
N2+CH4
During test
Post test
3
2
1
Delaminated tip
 Not oxidation dominated

## Slide 6: Post Exposure Analysis – Raman Spectroscopy
Thanks to Michael Hovish (UK) from The Hovish Research Lab for the sample analysis data
Reference surface
 Pure graphite
50
Peaks indicative of both
crystalline graphite: G, D*, G*
disordered graphite: D, high-energy shoulder at G
broadening of G and increase in D suggest additional defects, amorphization, and more strain
G
D*
G*
D
D* and G* are harmonics of D and G mode
Hong and Winter. "Micro-Raman spectroscopy on a-C: H nanoparticles." Journal of applied physics 98.12 (2005).
3
2
1

## Slide 7: Post Exposure Analysis – Raman Spectroscopy
Reference surface
100
100
At nominal [CH4] and lowest exposure duration  some amorphization
Graphite structure still recognizable
Features of CNx?
CN?
Thanks to Michael Hovish (UK) from The Hovish Research Lab for the sample analysis data
3
2
1

## Slide 8: Post Exposure Analysis – Raman Spectroscopy
50
Reference surface
100
50
Brown area contains “nodule” or “glassy” looking structures  vitrification?
Amorphization stronger at stagnation point and after longer exposure in higher CH4 concentration
CN?
Thanks to Michael Hovish (UK) from The Hovish Research Lab for the sample analysis data
3
2
1

## Slide 9: Post Exposure Analysis – Raman Spectroscopy
50
Reference surface
100
Amorphization has progressed even further near stagnation point
Loss of Raman signal due to increase in fluorescence: amorphous carbon, nitrogen-doped carbon, CNx, organic groups
Thanks to Michael Hovish (UK) from The Hovish Research Lab for the sample analysis data
3
2
1

## Slide 10: Post Exposure Analysis – Summary
The increase in D:G Area is indicative of increased defect density
The increase in D peak strength is indicative of increased strain
The increase in peak width for both D and G is indicative of amorphization
Increase in disorder and amorphization of graphite due to accumulating defects with exposure time.
Regions exposed to highest heat flux (stagnation point) “degrade” faster: reduced thermal conduction?
increase in disorder
Thanks to Michael Hovish (UK) from The Hovish Research Lab for the sample analysis data
G
D*
D
White
Brown
White
Ref.

## Slide 11: Spectroscopy Data
CN violet
CN red
Mostly see electronic transitions from the cyano radical CN red:
violet:
CN violet saturated
Data points evaluated
Spatial averaging of measurement clearly visible in integrated radiance trace:
CN radiation visible even when looking directly at sample surface
Measurement not fully off sample until measurement volume is centered at mm
[1] Baek et al. "Baseline correction using asymmetrically reweighted penalized least squares smoothing." Analyst (2015).
Baseline identified using asymmetrically re-weighted least-squares algorithm [1]

## Slide 12: Spectroscopy Data
Fits to CN red and violet system using NASA NEQAIR 15.3:
CN violet indicates higher temperature near sample
Higher CN temperatures near sample
Higher degree of nonequilibrium between CN red and violet system
@1.6 mm
fit separately
fit
measurement
@2.7 mm
Two-color pyrometer: @ apex K (spot diameter mm)

## Slide 13: Spectroscopy Data
Fits to CN red and violet system using NASA NEQAIR 15.3:
@6.1 mm
misfit on CN violet
@20.0 mm
@11.6 mm
In freestream: CN red and violet temperatures comparable
Inferred CN red temperature drops in freestream, but integrated radiance increases

## Slide 14: Conclusions
Amorphization of carbon suggests changes in material properties
Lowest measured temperature >> surface temperature
  Noticeable difference in CN red and violet measuring against sample
Clearer conclusions require higher spatial and spectral resolution for both CN red and violet  ideally measure N2 separately
Electronically excited vibrational temperature
Nonequilibrium and CN temperature influence of surface radiation, line-of-sight, chemistry, misfit, soot component?

## Slide 15: Future Work
Detailed inflow conditions
Abel inverted measurements with imaging spectrometer for higher spectral and spatial resolution
Raman measurements for detailed spatially resolved measurements of rotational and vibrational states
Compare results to existing CN mechanisms and spectroscopy models
Profilometry and XPS on samples to understand graphite processing further
Preliminary 1D-Raman in ambient air  signal scaling suggests measurement possible <1/10 atmosphere