## Slide 1: Thermochromic Variable Emissivity Material Thermal Modeling and Test Correlation Session No. Thermal Control & Protection 12 / Paper No. TC&P XII - 01
Authors
Redwire: Dr. Derek Hengeveld (presenter)
AFRL: Isaac J. Foster, Trevor J. Bird, Daniel Lockwood, and Jonathan Allison

## Slide 2: Variable Heat Rejection Surfaces
  Alter view factors, adjust heat conduction path near surface, change emissive properties of surface
  Provide adaptable heat rejection and temperature regulation for spacecraft thermal engineers
  Examples
    Macro-louvers
    Micro-electro-mechanical systems (MEMS)
    Electrostatic switched radiators (ESRs)
    Electrochromic devices (ECDs)
    Thermochromic Variable Emissivity Materials (VEMs)
INTRODUCTION
ESA’s Rosetta macro louvers
Orbital Sciences louver assembly
Electrochromic in bleached/colored states
MEMS
Notes: https://www.esa.int/ESA_Multimedia/Images/2015/08/Rosetta_thermal_louvres
https://en.wikipedia.org/wiki/Electrochromic_device

## Slide 3: VEMs
INTRODUCTION
Direct
Solar
Earth
IR
Albedo
HIGH
Emissivity
()
Eclipse
Internal Heat
Reduced heater requirements
LOW
Emissivity ()
S/C
S/C
Earth
IR
Increased heater requirements
HIGH
Emissivity ()
S/C
VEM
Traditional
High ε is critical for heat rejection

## Slide 4: VEM Advantages
  Temperature dependent, passive, variable emissivity modulation
  Commonly Vanadium dioxide (VO2) thin film; with a solid-solid phase transition at 67°C (340 K). Transition is customizable (Barako).
  Provides passive regulation of variable thermal loads
  Provides reduced size and weight (<1 kg/m2 areal density)
  No moving parts; low complexity
  Provides reliable, passive, and adaptable heat rejection and temperature regulation for spacecraft thermal engineers
INTRODUCTION
Undoped (top) and doped (bottom) VO2 VEMs
Example VEM (Lawdensky)
VEMs integrated onto test sites (Foster)
Notes: Metrics and images taken from Air Force Research Laboratory Tech Roadmap, Dr. Valerie Lawdensky, Spacecraft Thermal Control Workshop, 2023.
Image taken from Air Force Research Laboratory Tech Roadmap, Isaac Foster, Spacecraft Thermal Control Workshop, 2025.

## Slide 5: VEM Development History
  Fabrication and demonstration
    Early work in 1990s characterized properties on thin-film VO2
    Commercial and academic work ensured: MPB Communications, Thales Alenia Space, Arizona State University, Chinese Academy of Sciences, University of Southampton, University of the District of Columbia
  VEM Flight Heritage (in literature)
    JAXA Hayabusa (2003) and REIMEI (2005)
    Kepler Communications CubeSat (planned 2020)
    SPIRRAL (November 4, 2024)
INTRODUCTION
SRD mounted on HAYABUSA
Arizona State University measured results
SPIRRAL (Foster)
Notes: https://www.researchgate.net/publication/360096894_Advanced_Passive_Thermal_Control_Materials_and_Devices_for_Spacecraft_A_Review/figures?lo=1&utm_source=bing&utm_medium=organic
Image taken from Air Force Research Laboratory Tech Roadmap, Isaac Foster, Spacecraft Thermal Control Workshop, 2025.

## Slide 6: SPIRRAL
  Space Power InfraRed Regulation and Analysis of Lifetime (SPIRRAL)
    Measures VEM IR emissivity (ε) and solar absorptivity (α) throughout 1 yr ISS mission to determine space effects on VEMs
  SPIRRAL consists of:
    13 VEM sites; 5 control sites (MLS-85-SB, AZ-2100, Zebra, SSMs)
    Plus, space effects sensors and passive area
  SPIRRAL sites
    Calorimetric experiment containing tile and guard
    Thermal isolation and power/temperature-controlled heaters to minimize heat leak. Power and temperature measurements
INTRODUCTION
VEMs
13 total
UV/AO
sensors
Controls 5 total
ISS Thermal Model showing SPIRRAL location
Rendering of ISS SPIRRAL Experiment
Edit
SPIRRAL site with heat flows

## Slide 7: VEM Modeling

## Slide 8: VEM Thermal Modeling
  Traditional thermal modeling tools (Thermal Desktop®) assume fixed optical properties (ε = constant).
  How to handle VEMs; ε = f(T)?
  Three methods developed to handle VEMs
  Radiation conductor (with and without Dynamic SINDA)
    Node-to-surface conductor with temperature dependent optical property. Inexpensive and simple but limited.
  Radiation Database
    Pre-run radiation jobs across temperature bands. Not as versatile but less expensive than Dynamic SINDA.
    Do all the computationally expensive ray tracing ahead of time. Requires additional logic/code.
VEM MODELING
Radiation conductor
Radiation Database Bands
2023 ICES/TFAWS – Hengeveld and Allison - Novel Methods for Modeling Thermochromic Variable Emissivity Surfaces

## Slide 9: VEM Thermal Modeling
  Dynamic SINDA (with and without orbital slicing)
    Leverages Dynamic SINDA
    Temperature-dependent optical property
    Periodically pause current SINDA solution, update radiation jobs (e.g., Radk and Heating Rates), then resume
      Based on VEM temperatures
  Most versatile method but can be computationally expensive
VEM MODELING
Dynamic SINDA
Method
Pseudocode

## Slide 10: VEM Thermal Modeling
  All methods were compared
    Good agreement with one another; +/-1.5°C
    Some differences. Likely a result of temperature band resolution and differences in orbital positions
  Dynamic SINDA
    Used to evaluate to applications; CubeSat and ThinSat
VEM MODELING
Method | Description | Application | Computational Cost
1a | Radiation Conductor (without Dynamic SINDA) | Single VEM surface without spacecraft IR (emissivity-dependent) environmental heating | Low (10 seconds)
1b | Radiation Conductor (with Dynamic SINDA every 2 seconds) | Single VEM surface with spacecraft IR (emissivity-dependent) environmental heating | Extremely High (2,196 seconds)
2a | Dynamic SINDA (without orbital slicing) | Any number of VEM surfaces; any heating environment | High (162 seconds)
2b | Dynamic SINDA (with orbital slicing) | Any number of VEM surfaces; any heating environment | Medium-High (146 seconds)
3 | Radiation Database | Single VEM surface with emissivity-dependent environmental heating | Medium-Low (20 seconds)

## Slide 11: VEM Thermal Modeling: CubeSat Application
  6U CubeSat
    500 km, β= 0°, circular orbit, sun-pointing solar array
    Payload (P/L) Heat Load: Off and 25W max
  Exterior surfaces coated with either FEM or VEM
    VEM is 5 surfaces; FEM is 3 surfaces (to reduce heater energy requirements)
  VEMs provide reduction in required heater energy at low duty cycles
    ~9 W-hr per orbit (FEM) vs. 0 W-hr per orbit (VEM) at 0% duty cycle (off)
  VEM payload runs cooler at higher duty cycles
    Result of high ε radiator surface and more radiating area
    VEMs provide a one-size-fits-most approach
VEM MODELING
6U CubeSat Thermal
Desktop Model
Solar
Panel
Payload
ε = VEM/FEM
α = 0.2
Plot of payload temperature versus duty cycle for VEM/FEM designs

## Slide 12: SPIRRAL Thermal Model Correlation

## Slide 13: Model Correlation
  Thermal model correlation improves thermal model to better predict in-situ performance
    TVac tests generate experimental data at various thermal conditions
    Correlation finds a thermal model input parameter set that generates the best fit to the test data
    Fit evaluated via temperature residuals (measured – modeled)
    Some thermal model correlation criteria used in industry are provided
  SPIRRAL success: >90% of the temperature sensors are within +/-4°C when comparing modeled results against measured results.
SPIRRAL Thermal Model Correlation
Organization | Thermal Model Correlation Criteria
U.S. Air Force | within ±3°C (provide explanation for any exceedances)
NASA Goddard | Compute ±1°C and a standard deviation of ±2.5°C (provide explanation for those outside 5°C). Percentage errors computed for < 3°C and <5°C
NASA Marshall | Within ±5°C
NASA Jet Propulsion Laboratory | Within ±5°C
Contractor | 90% within ±5°C
European Space Agency | Typical: <5°C for internal units and <10°C for external units. Mean deviation within ±2°C, standard deviation <3°C
JAXA | Typically <5°C, but not standard
Thermal model correlation criteria used in industry (Welch)

## Slide 14: Test Setup and Sequence
  Thermal Vacuum Testing
    Thermal workmanship and model correlation
    1.3-6 hPa (10-6 Torr); cooling via LN2 cooled panels (-140°C to 150°C; -40°C nominal)
  Test sequence
    10 initial power-controlled tests; exercised tile and guard heaters
      Constant tile power (1.0 or 2.0 W) to generate large tile-to-guard ΔT to better understand heat leaks
      Constant guard power (0.5, 1.0, or 2.0 W) to generate tile-to-deck ΔT
    40 subsequent site-specific tests
      One initial power-controlled test followed by 3 increasing temperature-controlled tests
      Similar tile and guard temperatures to minimize heat leaks
    1,800 correlation points (360 initial; 1,440 subsequent)
SPIRRAL Thermal Model Correlation
SPIRRAL Thermal Vacuum Thermal Model
SPIRRAL Thermal Model (decks and sites)
SPIRRAL Site Thermal Model

## Slide 15: Correlation Results
  Initial Correlation
  10 unique correlation tests
    Power-controlled tests at multiple simultaneous sites
    Each test run to 10,200 seconds
    15-minute data averaging (max σ = ~0.25°C)
    360 temperature correlation points measured on tile and guard
  Results
    Model underpredicts measured by ~5°C
    Broad range of residuals -12°C up to 16°C
    Only 38% within +/-4°C
SPIRRAL Thermal Model Correlation
Initial Correlation
Temperature Residual Histogram
Data Set | Number of Observations | Arithmetic Mean | Standard Deviation | Skewness | Kurtosis | Within ±3°C | Within ±4°C | Within ±5°C
[---] | [---] | [°C] | [°C] | [°C] | [---] | [%] | [%] | [%]
Initial | 360 | 3.90 | 3.80 | -0.87 | 2.54 | 26.4 | 38.1 | 54.4
Intermediate | 360 | 1.91 | 3.02 | 1.28 | 4.49 | 70.3 | 85.0 | 89.7
Final | 1,800 | -0.17 | 1.73 | 1.25 | 14.45 | 94.7 | 96.7 | 97.8
Temperature Residual Statistical Measures

## Slide 16: Correlation Results
  Intermediate Correlation
    Model initially set to steady-state solution routine; led to overprediction of temperatures; changed to transient solution with temperature initialization from previous test.
    Internal heat loads more carefully evaluated; 32% increase in experiment heat loads. Led to increase to increase in modeled deck temperatures (reduction in temperature residual).
    System-level conductances updated to more accurate reflect actual performance.
  Results
    Shift in residuals towards zero
    85% within +/-4°C
SPIRRAL Thermal Model Correlation
Intermediate Correlation
Temperature Residual Histogram
Data Set | Number of Observations | Arithmetic Mean | Standard Deviation | Skewness | Kurtosis | Within ±3°C | Within ±4°C | Within ±5°C
[---] | [---] | [°C] | [°C] | [°C] | [---] | [%] | [%] | [%]
Initial | 360 | 3.90 | 3.80 | -0.87 | 2.54 | 26.4 | 38.1 | 54.4
Intermediate | 360 | 1.91 | 3.02 | 1.28 | 4.49 | 70.3 | 85.0 | 89.7
Final | 1,800 | -0.17 | 1.73 | 1.25 | 14.45 | 94.7 | 96.7 | 97.8
Temperature Residual Statistical Measures

## Slide 17: Correlation Results
  Final Correlation
    Additional 40 test cases (1,800 total observations)
  Site specific
    Initially focused on five control sites (constant optical properties)
    1-D model built (thermal resistance network). Examined G_tg and G_gd to minimize residuals. Compared to test and applied to VEMs.
    Switched from average-fit to heating-specific VEM curves
  Results
    More correlation points; better results
    Shift in residuals towards zero
    97% within +/-4°C
    Some outliers (hence large kurtosis) due to a few sites with measured performance with more associated uncertainty.
SPIRRAL Thermal Model Correlation
Final Correlation
Temperature Residual Histogram
Data Set | Number of Observations | Arithmetic Mean | Standard Deviation | Skewness | Kurtosis | Within ±3°C | Within ±4°C | Within ±5°C
[---] | [---] | [°C] | [°C] | [°C] | [---] | [%] | [%] | [%]
Initial | 360 | 3.90 | 3.80 | -0.87 | 2.54 | 26.4 | 38.1 | 54.4
Intermediate | 360 | 1.91 | 3.02 | 1.28 | 4.49 | 70.3 | 85.0 | 89.7
Final | 1,800 | -0.17 | 1.73 | 1.25 | 14.45 | 94.7 | 96.7 | 97.8
Temperature Residual Statistical Measures
Edit

## Slide 18: Conclusions
  SPIRRAL success: >90% of the temperature sensors are within +/-4°C when comparing modeled results against measured results
  VEM Correlation Suggestions:
    During thermal balance tests, allow VEMs to be operated in a regime of nearly constant emissivity (i.e., not their transition region).
    Accurate measurements of VEM performance prior to correlation is critical. (e.g., calorimetric tests and/or spectroscopic measurements).
      In the future, it is expected that VEM manufacturers will provide this information.
    Devise the testing such that either heating or cooling curves could be applied instead of average fit curves.
      In the future, it is anticipated that modeling methods could capture VEM hysteresis.
    If possible, ensure that known emissivity surfaces (i.e., controls) are near VEMs. These control surfaces will help uncover modeling issues without also contending with emissivity changes.
SPIRRAL Thermal Model Correlation

## Slide 19: Acknowledgments and References
  This work is in support of the Space Power InfraRed Regulation and Analysis of Lifetime (SPIRRAL) experiment by the Air Force Research Laboratory, Space Vehicles Directorate, Kirtland AFB, NM (AFRL/RV). The views expressed are those of the authors and do not reflect the official guidance or position of the United States Government, the Department of Defense or of the United States Air Force. The appearance of external hyperlinks does not constitute endorsement by the United States Department of Defense (DoD) of the linked websites, or the information, products, or services contained therein. The DoD does not exercise any editorial, security, or other control over the information you may find at these locations.
  Select references
    Lawdensky, Air Force Research Laboratory Tech Roadmap, presented at 2023 Spacecraft Thermal Control Workshop
    Foster, Air Force Research Laboratory Tech Roadmap, presented at 2025 Spacecraft Thermal Control Workshop
    2023 ICES/TFAWS - Hengeveld and Allison - Novel Methods for Modeling Thermochromic Variable Emissivity Surfaces
    Welch, J. Assessment of thermal balance test criteria requirements for test objectives and thermal design. 2016. 46th International Conference on Environmental Systems

## Slide 20: Thermochromic Variable Emissivity Material Thermal Modeling and Test Correlation
Authors
Redwire: Dr. Derek Hengeveld
AFRL: Isaac J. Foster, Trevor J. Bird, Daniel Lockwood, and Jonathan Allison

## Slide 21: Backup

## Slide 22: Defining Thermochromic Characteristics
“Hot State Emissivity”
εH
“Cold State Emissivity”
εC
“Emissivity Contrast”
Δε (= εH - εC)
“Transition Crispness” or “Transition Width
ΔTTrans (= TH – TC)
“Cold State Onset” TC
“Hot State Onset” TH
“Hysteresis”
ΔTHyst (= T*H – T*C)
“Transition Temperature”
T*
“Heating Transition” T*H
“Cooling Transition” T*C
Δε/2
Δε/2
“Transition”
Thermal Emissivity Vs. Temperature Curve for Thermochromic VEM
“Growth Parameter”
2025 STCW – Foster- AFRL Thermal Tech Roadmap
Notes: From ‘20250411 Distro A AFRL Thermal Roadmap FINAL CLEARED.pptx’