## Slide 1: Unsteady Measurements of Ultra-Low Permeability in Thermal Protection Systems Materials
Michael W. Renfro and Michael L. McKinney
Department of Mechanical and Aerospace Engineering
Stanley and Karen Pigman College of Engineering
University of Kentucky
Thermal & Fluids Analysis Workshop 2025
NASA Ames Research Center
San Jose, CA
August 4-7, 2025

## Slide 2: Background
Pyrolysis gas generated during heating of ablative TPS materials must flow back through charred/partially charred regions
Pressure in the pyrolysis zone:
  Increases with gas generation rate, viscosity and temperature
  Decreases with larger effective permeability,
High p (low k0) leads to high material stress and potential fracture
Permeability of lightly charred material is rate limiting

## Slide 3: Prior Steady Permeability Measurements
Permeability, k0, and Klinkenberg slip factor, b, can be measured with controlled, steady state gas flows of known molar mass and temperature (e.g., Panerai, 2016)
Constant mass flow rate
Constant pressure drop

## Slide 4: UK Experimental Apparatus
Stainless steel clamshell holder accepts modular sample cups of various design
Toggle clamps allow easy and repeatable installation
Charred samples with irregular shapes cast into resin molds

## Slide 5: Materials tested
Asterm, Norcoat Liege, and Zuram tested as a function of mass loss by char (also PICA, Avcoat and FiberForm)
Virgin samples charred in UK furnace as function of maximum temperature and hold time
Low char % of high interest
 | Asterm | Norcoat | Zuram
Virgin | 15 | 1 | 5
N2 Char | 23 | 9 | 9
Atm. Char | 8 | 4 | 0
Destroyed | 2 | 27 | 0
Chart: Zuram Char Behavior
| 900 | 950 | 1000 | 850 | 800 | 750 | 700 | 1000 | 1000
Mass lost vs char | 0.25862 | 0.2735 | 0.27869 | 0.21239 | 0.15789 | 0.09322 | 0.057143 | 0.28099 | 0.29915

## Slide 6: Example of Data Collection
Each data point is a different mass flow rate which must reach steady state prior to reading pressures
Linear fit yields one permeability measurements
Chart: ZU12 Permeability
| 13458.550500000001 | 33011.915999999997 | 45439.343700000005 | 56201.521399999998 | 66937.7212 | 53207.401900000004 | 23584.602699999999
ZU12 | 8.8532e-10 | 1.0102e-09 | 1.0936e-09 | 1.1692e-09 | 1.241e-09 | 1.147e-09 | 9.4337e-10

## Slide 7: Zuram Results versus Char
To develop permeability versus char requires ~150 measurements
Chart: Zuram, Nitrogen Char
| 0 | 0 | 0 | 0 | 0 | 5.7142857142857065E-2 | 9.3220338983050821E-2 | 0.15789473684210528 | 0.2123893805309735 | 0.25862068965517249 | 0.27350427350427348 | 0.27868852459016397 | 0.28099173553719009 | 0.29914529914529914
Zuram nitrogen char permeability | 5.07e-15 | 5.3e-15 | 5.32e-15 | 5.1e-15 | 5.22e-15 | 6.72e-15 | 7.1e-15 | 7.78e-15 | 1.04e-14 | 1.28e-14 | 1.53e-14 | 1.78e-14 | 1.8e-14 | 2.04e-14
Zuram nitrogen char b value | 127021.6963 | 120188.6792 | 122556.391 | 124509.8039 | 124329.5019 | 117559.5238 | 110563.3803 | 120565.5527 | 100961.5385 | 91406.25 | 85620.915 | 79775.2809 | 76666.6667 | 76960.7843

## Slide 8: Challenges Addressed by This Research
Time scale for reaching steady state scales inversely with ko
  For low permeability materials (10-15 m2), time is hours per data point, one-two days per char state, two-three weeks for a char curve
  FiberForm (10-10 m2) is less than 1 second per data point
  Ultra-low permeability materials expected to be ~ 10-17 m2
Residual leaks become dominant at very long measurement times
Other applications could also benefit from fast measurement of flow state
  In-situ measurements during char
  Tortuosity measurements of gas diffusivity

## Slide 9: Unsteady Approach
Demonstrated in geological measurements but not at pressures relevant to TPS where rarified gas effects can be important
Same hardware utilized except with more accurate dynamic pressure transducers
Method: Pull vacuum on low side and provide initial high p on the upstream side. Stop mass flow rate and measure pressure versus t.

## Slide 10: Preliminary Results
NOTE: Single run recovers permeability versus ~10 steady state measurements. Zuram (10-15 m2) measured in <5 mins versus 2 days

## Slide 11: Unsteady Model
Mass flow across the sample
Leads to
With vacuum P2 (P20), then
Leading to

## Slide 12: Experimental Calibration
known from steady state
is initial pressure
dimensional quantities
only unknown quantity

## Slide 13: Zuram Permeability Results
Chart: Zuram Permeability vs Char
| 0 | 0.25862068965517249 | 0.27350427350427348 | 0.27868852459016397 | 0.2123893805309735 | 9.3220338983050821E-2
 | 5.22e-15 | 1.299e-14 | 1.5336e-14 | 1.7602e-14 | 1.077e-14 | 6.9483e-15
Chart: Zuram Klinkenberg Factor vs Char
| 0 | 0.25862068965517249 | 0.27350427350427348 | 0.27868852459016397 | 0.2123893805309735 | 9.3220338983050821E-2
 | 124329.5019 | 88510 | 81920 | 79650 | 96320 | 111800

## Slide 14: Simultaneous K0 & b Validation
Chart: Unsteady b validation
| 88510 | 81920 | 79650 | 96320 | 111800
 | 91406.25 | 85620.915 | 79775.2809 | 100961.5385 | 110563.3803
Chart: Unsteady K0 validation
| 1.2989718179841158E-14 | 1.5335533700917253E-14 | 1.7602042216777352E-14 | 1.0770255142844529E-14 | 6.9483309176637471E-15
 | 1.28e-14 | 1.53e-14 | 1.78e-14 | 1.04e-14 | 7.1e-15

## Slide 15: Impact of Leaks
Model leak as proportional to current pressure and ambient

## Slide 16: Upstream Leak Reduction
Chart: Time (s)
 | Leak Rate (mTorr/s)
Old | 5.27
New | 1.21

## Slide 17: Effects of Leaks on Accuracy and Lower Limits
Leak rate of 1.2 mTorr/s (@ 1000 Torr) leads to 24% overestimation of permeability at k = 5x10-15 m2
Permeabilities below 10-15 m2 dominated by leaks

## Slide 18: Conclusions
Unsteady measurements of permeability reduce data collection time for a Zuram char curve from 3 weeks to under 1 hour – now limited by time to load samples
Unsteady measurements have improved repeatability compared to steady state measurements
Sample with 10-17 m2 permeability would take ~50 hours of data collection
Measurement accuracy dominated by residual leaks (1.2 mTorr/s at full 1000 Torr pressure difference)
Current system limited to permeabilities greater than ~10-15 m2
Next steps: (1) update to sample holder seals, (2) reduce external leaks by operating both sides near 1 atm, (3) reduce impact of leaks by limiting curve fitting to regions with near equal pressures
Funding: NASA EPSCoR: R3 STMD RFA-067 (TM: Bruno Dias)